12-7

Polymers

Description:  Show examples of common synthetic organic polymers to encourage thought / discussion about differences.

Concept:  Properties of polymers depend on crystallinity and length of carbon chain.

Materials:

- Saran wrap

- polyethylene garbage bags and food container

- PVC pipe

- Lucite bar

- Teflon sheet

Procedure:  Pass samples to students or display on Elmo Presenter.

Notes:  Developed for Prof. Ewing's C100 Course.